Piezoelectric Performance Enhancement in KNN-Based Piezoceramics: Origins behind the PPT Effects

Author A 1, Author B2*, Author C1

1. School of Materials Science and Engineering, Tsinghua University, Beijing, China

* Corresponding author: jingfeng@mail.tsinghua.edu.cn

Key words: Potassium-sodium niobate; Phase coexistence; Lattice softening; Large Piezoelectricity; Temperature stability;

Due to growing concerns on environment and human health, the development of the lead-free piezoelectrics has drawn significant attention. Searching for lead-free ceramics with high piezoelectricity to meet the requirements of the industrial applications has always been a prime aim in this scientific field. Furthermore, the mechanism for property enhancement in lead-free piezoceramics is a hot topic but still controversial. In this work, we developed a new KNN-based lead-free ceramic material which afforded a large d33 over 500 pC/N and a high Tc ~200 oC. Apart from the property improvement from phase transition effects, we found additional contributions for the superior piezoelectric response, i.e. the composition-induced structural instability. This composition-induced structural instability which significantly enhances piezoelectricity even in absence of a phase transition can result from the reduced tetragonality (c/a) and more covalent lattice matrix. Hierarchical domain structure was observed in KNN-based piezoelectric materials by Transmission Electron Microscopy (TEM). Nano-size domains were found in side of submicron domains, further corroborating the structural instability in a microscopic perspective. These findings may provide new insight into the further enhancement of the properties in KNN-based ceramics. The future inspired work might break the bottleneck and bring the d33 value to a new height.

# Text boxes

姓前名后，姓全大写，名首字母大写,通讯作者后加星号(*)

Full surname before first name in abbreviation, corresponding author should be indicated with *

题目后空一行, 12号字, 加粗

Skip a line after title, 12pt font size, bold.

14号字, 加粗, 单词首字母大写

Use 14pt font size, bold, capitalize the first letter of each word.

全文采用 times new roman 字体

Full text in times new roman font

2.5 cm

2.0 cm

12号字

12pt font size